## Slide 1: Fano-resonant metasurfaces for virus sensing application
H3 Oral Defence
Kushagra Shrivastava
Beertino Romerow Woe
National Junior College
Chu Hong-Son
IHPC, A*STAR

## Slide 2
H3 Research
Kushagra Shrivastava
1
Contents
Introduction
Experiments and Methodology
Results and Discussion
Future Works

## Slide 3
H3 Research
Kushagra Shrivastava
2
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Deadly Viruses
COVID-19
SARS
Ebola

## Slide 4
H3 Research
Kushagra Shrivastava
3
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Methods of Virus Detection
Reverse Transcription – Polymerase Chain Reaction
Afzal, A. (2020). Molecular diagnostic technologies for COVID-19: Limitations and challenges. Retrieved from: https://dx.doi.org/10.1016%2Fj.jare.2020.08.002
False
Results
4 – 6 hours analysis time
Notes: ART test works on a similar idea

## Slide 5
H3 Research
Kushagra Shrivastava
4
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Metasurfaces
Subwavelength thickness
Optical antennae on top
Chen, H. T. (2016). A review of metasurfaces: physics and applications. Retrieved from: https://doi.org/10.1088/0034-4885/79/7/076401

## Slide 6
H3 Research
Kushagra Shrivastava
5
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Metasurfaces
Chen, H. T. (2016). A review of metasurfaces: physics and applications. Retrieved from: https://doi.org/10.1088/0034-4885/79/7/076401
Notes: Binding the virus to the metasurface

## Slide 7
H3 Research
Kushagra Shrivastava
6
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Metasurfaces
Based on resonance due to structure
Small changes in the environment can have drastic effects
Chen, H. T. (2016). A review of metasurfaces: physics and applications. Retrieved from: https://doi.org/10.1088/0034-4885/79/7/076401

## Slide 8
H3 Research
Kushagra Shrivastava
7
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Fano Resonance
Limonov, M., Rybin, M., Poddubny, A., Kivshar, Y. (2017). Fano resonances in photonics. Retrieved from: http://dx.doi.org/10.1038/nphoton.2017.142

## Slide 9
H3 Research
Kushagra Shrivastava
8
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Fano Resonance
Limonov, M., Rybin, M., Poddubny, A., Kivshar, Y. (2017). Fano resonances in photonics. Retrieved from: http://dx.doi.org/10.1038/nphoton.2017.142
Sudden shift between a dip and rise
Sharp resonance peaks
Biosensing application

## Slide 10
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Aim
To create a structure that is highly sensitive to minute changes in refractive index in its local surroundings, so that it can quickly detect low concentrations of viruses using Fano resonance
9

## Slide 11
Experiments and methodology

## Slide 12
H3 Research
Kushagra Shrivastava
10
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Lumerical-FDTD
Finite Difference Time Domain method is a computational method to solve Maxwell’s Equations
Taflove, A., & Hagness, S. (2010). Computational electrodynamics. Boston, Mass: Artech House.

## Slide 13
H3 Research
Kushagra Shrivastava
11
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Structure Idea
Structure adopted from Yang et al.’s work on Fano resonance
Yang, L., Yu, S., Li, H., Zhao, T. (2021) Multiple Fano resonances excitation on all-dielectric nanohole arrays metasurfaces. Retrieved from: https://doi.org/10.1364/OE.419941
Notes: Structure and wavelength relation

## Slide 14
H3 Research
Kushagra Shrivastava
12
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Experimental Metasurface
SiO2 Substrate
Etched Si Chip
Plane wave source
Transmission Monitor
Simulation Region
Refractive index:1.33

## Slide 15
H3 Research
Kushagra Shrivastava
13
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Experimental Metasurface
Runs on EM waves with wavelengths 900 nm to 1300 nm

## Slide 16
H3 Research
Kushagra Shrivastava
14
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Dimensions

## Slide 17
H3 Research
Kushagra Shrivastava
14
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Dimensions
510 nm
510 nm

## Slide 18
H3 Research
Kushagra Shrivastava
15
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Dimensions
h
h was altered from 60 nm to 160 nm

## Slide 19
H3 Research
Kushagra Shrivastava
16
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Dimensions
I
II
III
IV
dl
dl
d0
d0
dl was altered from 20 nm to 170 nm
d0 was kept constant at 80 nm

## Slide 20
H3 Research
Kushagra Shrivastava
17
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Virus simulation
Virus changes the local surface refractive index, causing a shift in resonant peaks

## Slide 21
H3 Research
Kushagra Shrivastava
18
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Liquid Layer
Varying Dimensions | Benchmark for best dimensions
1.34 | 1.34 – 1.40
Δ Concentration of viruses ≡ Δ Refractive index of liquid layer

## Slide 22
Results and discussion

## Slide 23
H3 Research
Kushagra Shrivastava
19
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Principle of data analysis
Better sensor
Large shift in spectrum with sharp peaks

## Slide 24
H3 Research
Kushagra Shrivastava
20
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Altering dl
Redshift increased as dl increased

## Slide 25
H3 Research
Kushagra Shrivastava
21
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Altering dl
4.28 nm
12.5 nm
9.80 nm
16.6 nm
4.26 nm
12.2 nm
9.20 nm
16.2 nm
Redshift decreased at 170 nm
dl = 160 nm is better

## Slide 26
H3 Research
Kushagra Shrivastava
22
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Altering h
No Fano resonance

## Slide 27
H3 Research
Kushagra Shrivastava
23
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Altering h
h = 120 nm has the least peak width
Increasing width with similar redshift
Notes: Overlaps between the peaks

## Slide 28
H3 Research
Kushagra Shrivastava
24
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor dimensions
As per the last two experiments, h = 120 nm with
dl = 160 nm will yield the best working sensor

## Slide 29
H3 Research
Kushagra Shrivastava
25
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor Benchmarks (h = 120 nm, dl = 160 nm)
Zhang, S., Wong, C., Zeng, S., Bi, R., Tai, K., Dholakia, K., & Olivo, M. (2020). Metasurfaces for biomedical applications: imaging and sensing from a nanophotonics perspective. Retrieved from: https://doi.org/10.1515/nanoph-2020-0373
Sensitivity
Measurement of how responsive sensor is to changes in refractive index
Resonant Wavelength
Local refractive index

## Slide 30
Sensitivity
H3 Research
Kushagra Shrivastava
26
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor Benchmarks (h = 120 nm, dl = 160 nm)

## Slide 31
H3 Research
Kushagra Shrivastava
27
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor Benchmarks (h = 120 nm, dl = 160 nm)
Sensitivity
Mode I
Mode II
Mode III
Mode IV

## Slide 32
H3 Research
Kushagra Shrivastava
28
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor Benchmarks (h = 120 nm, dl = 160 nm)
Afzal, A. (2020). Molecular diagnostic technologies for COVID-19: Limitations and challenges. Retrieved from: https://dx.doi.org/10.1016%2Fj.jare.2020.08.002
Measures the resolution and sensing potential of the sensor
Sensitivity
Full Width at Half Maximum
Figure of Merit (FOM)
Notes: Make reference to the benchmark for other tests

## Slide 33
H3 Research
Kushagra Shrivastava
29
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Sensor Benchmarks (h = 120 nm, dl = 160 nm)
Figure of Merit (FOM)

## Slide 34
H3 Research
Kushagra Shrivastava
30
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Analysis of the Benchmarks
Sensitivity: 229.46 nm/RIU
FOM: 59.04
Mode II is the best performing mode out of all the modes

## Slide 35
H3 Research
Kushagra Shrivastava
31
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Analysis of the Benchmarks
Lee, K., Huang, J., Chang, J., Wu, S., Weia, P. (2015). Ultrasensitive Biosensors Using Enhanced Fano Resonances in Capped Gold Nanoslit Arrays. Retrieved from: https://dx.doi.org/10.1038%2Fsrep08547
Li, N., Xu, Z., Dong, Y., Hu, T., Zhong, Q., & Fu, Y. et al. (2020). Large-area metasurface on CMOS-compatible fabrication platform: driving flat optics from lab to fab. From: https://doi.org/10.1515/nanoph-2020-0063
Other metasurface sensors have reached sensitivity up to 962 nm/RIU
Lower performance than other new sensors, but Si wafers cheaper and more efficient to manufacture (Si CMOS)

## Slide 36
H3 Research
Kushagra Shrivastava
32
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Overall Analysis
My research discovered sensor with dl=160 nm and h=120 nm, working on wavelengths of mode II, was the best performing sensor, with high sensitivity and
Figure of Merit
Notes: Make this more interesting

## Slide 37
Future works

## Slide 38
H3 Research
Kushagra Shrivastava
33
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Future works
Engineering of the sensor with the abovementioned dimensions
Verification of the structure model by real experiment if possible
Notes: Need to come out of the project – validation of the results

## Slide 39
Thank you

## Slide 40
References
[1] Page, J. (2021). In Hunt for Covid-19 Origin, Patient Zero Points to Second Wuhan Market. Retrieved from https://www.wsj.com/articles/in-hunt-for-covid-19-origin-patient-zero-points-to-second-wuhan-market-11614335404
[2] Adhanom, T. (2020). WHO Director-General's opening remarks at the media briefing on COVID-19. Retrieved from https://www.who.int/director-general/speeches/detail/who-director-general-s-opening-remarks-at-the-media-briefing-on-covid-19---11-march-2020
[3] Ozili, P., Arun, T. (2020). Spillover of COVID-19: Impact on the Global Economy. Retrieved from https://dx.doi.org/10.2139/ssrn.3562570
[4] Ritchie, H., Mathieu, E., Rodés-Guirao, L., Appel, C., Giattino, C., Ortiz-Ospina, E., Hasell, J., Macdonald, B., Beltekian, D., Roser, M. (2020). Coronavirus Pandemic (COVID-19). Retrieved from https://ourworldindata.org/coronavirus-data
[5] Mohapatra, R., Pintilie, L., Kandi, V., Sarangi, A., Das, D., Sahu, R., Perekhoda, L. The recent challenges of highly contagious COVID-19, causing respiratory infections: Symptoms, diagnosis, transmission, possible vaccines, animal models, and immunotherapy. Retrieved from https://dx.doi.org/10.1111%2Fcbdd.13761
[6] Jawerth, N. (2020). How is the COVID-19 virus detected using real time RT–PCR? Retrieved from: https://www.iaea.org/bulletin/infectious-diseases/how-is-the-covid-19-virus-detected-using-real-time-rt-pcr#:~:text=This%20technique%20allows%20scientists%20to,detecting%20the%20COVID%2D19%20virus.
[7] Afzal, A. (2020). Molecular diagnostic technologies for COVID-19: Limitations and challenges. Retrieved from: https://dx.doi.org/10.1016%2Fj.jare.2020.08.002
[8] GE Healthcare launches next generation Biacore (TM) molecular interaction analysis platform | GE News. (2016). Retrieved from https://www.ge.com/news/press-releases/ge-healthcare-launches-next-generation-biacoretm-molecular-interaction-analysis
[9] Label-Free Silicon Chip based Biosensing – Omega Optics. Retrieved from http://omegaoptics.com/technologies/label-free-silicon-chip-based-biosensing/
[10] Chen, H. T. (2016). A review of metasurfaces: physics and applications. Retrieved from: https://doi.org/10.1088/0034-4885/79/7/076401
[11] Escobedo, C. (2013). On-chip nanohole array based sensing: A review. Retrieved from: http://dx.doi.org/10.1039/c3lc50107h
[12] Amina, M., Siddiquia, O. Abutarbousha, H. Farhatb, M. Ramzanc, R. (2021). A THz graphene metasurface for polarization selective virus sensing. Retrieved from: https://doi.org/10.1016/j.carbon.2021.02.051
[13] Liu, L., Li, T., Liu, Z., Fan, F., Yuan, H., & Zhang, Z. et al. (2020). Terahertz polarization sensing based on metasurface microsensor display anti-proliferation of tumor cells with aspirin. Biomedical Optics Express. Retrieved from: https://doi.org/10.1364/boe.392056
[14] Li, Z., Zhu, Y., Hao, Y., Gao, M., Lu, M., Stein, A., Park, A., Hone, J., Lin, Q., Yu, N., (2019) Hybrid Metasurface-Based Mid-Infrared Biosensor for Simultaneous Quantification and Identification of Monolayer Protein. Retrieved from: https://doi.org/10.1021/acsphotonics.8b01470
[15] Limonov, M., Rybin, M., Poddubny, A., Kivshar, Y. (2017). Fano resonances in photonics. Retrieved from: http://dx.doi.org/10.1038/nphoton.2017.142
[16] Xu, R., Zhang, Z., Wieck, A., Jukam, M. (2020). Terahertz Fano resonances induced by combining metamaterial modes of the same symmetry. Retrieved from: https://doi.org/10.1364/OE.383713
[17] Pathania, P., Shishodia, M. (2021). Fano Resonance-Based Blood Plasma Monitoring and Sensing using Plasmonic Nanomatryoshka. Retrieved from: https://dx.doi.org/10.1007%2Fs11468-020-01343-z
[18] Lee, K., Huang, J., Chang, J., Wu, S., Weia, P. (2015). Ultrasensitive Biosensors Using Enhanced Fano Resonances in Capped Gold Nanoslit Arrays. Retrieved from: https://dx.doi.org/10.1038%2Fsrep08547
[19] Hajebifard, A., Berini, P. (2017). Fano resonances in plasmonic heptamer nano-hole arrays. Retrieved from: https://doi.org/10.1364/OE.25.018566

## Slide 41
References
[20] Huang, T., Zeng, S., Zhao, X., Cheng, Z., Shum, P. (2018) Fano Resonance Enhanced Surface Plasmon Resonance Sensors Operating in Near-Infrared. Retrieved from: https://doi.org/10.3390/photonics5030023
[21] Yang, L., Yu, S., Li, H., Zhao, T. (2021) Multiple Fano resonances excitation on all-dielectric nanohole arrays metasurfaces. Retrieved from: https://doi.org/10.1364/OE.419941
[22] Palik, E. (1985). Handbook of optical constants of solids. Orlando: Academic Press.
[23] Ansys Insight: Diverging Simulations. (2021). Retrieved from https://forum.ansys.com/discussion/25566/ansys-insight-diverging-simulations
[24] Rumble, J. (2021). CRC HANDBOOK OF CHEMISTRY AND PHYSICS (102nd ed.). [S.l.]: CRC PRESS.
[25] Zhang, S., Wong, C., Zeng, S., Bi, R., Tai, K., Dholakia, K., & Olivo, M. (2020). Metasurfaces for biomedical applications: imaging and sensing from a nanophotonics perspective. Retrieved from: https://doi.org/10.1515/nanoph-2020-0373
[26] Mi, Q., Sang, T., Pei, Y., Yang, C., Li, S., Wang, Y., Ma, B. (2021). High-quality-factor dual-band Fano resonances induced by dual bound states in the continuum using a planar nanohole slab. Retrieved from: https://doi.org/10.1186/s11671-021-03607-x
[27] Li, N., Xu, Z., Dong, Y., Hu, T., Zhong, Q., & Fu, Y. et al. (2020). Large-area metasurface on CMOS-compatible fabrication platform: driving flat optics from lab to fab. Retrieved from: https://doi.org/10.1515/nanoph-2020-0063
[28] UCSB Science Line. (2014). Retrieved from http://scienceline.ucsb.edu/getkey.php?key=4527
[29] Barchiesi, D., Kessentini, S., Guillot, N., de la Chapelle, M., & Grosges, T. (2013). Localized surface plasmon resonance in arrays of nano-gold cylinders: inverse problem and propagation of uncertainties. Retrieved from: https://doi.org/10.1364/oe.21.002245

## Slide 42
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Fano Resonance
Limonov, M., Rybin, M., Poddubny, A., Kivshar, Y. (2017). Fano resonances in photonics. Retrieved from: http://dx.doi.org/10.1038/nphoton.2017.142
Strong damping
Weak damping

## Slide 43
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Fano Resonance
Limonov, M., Rybin, M., Poddubny, A., Kivshar, Y. (2017). Fano resonances in photonics. Retrieved from: http://dx.doi.org/10.1038/nphoton.2017.142
For metasurfaces, resonance is between the surface and external radiation

## Slide 44
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
How does FDTD work? – Yee Cell
Taflove, A., & Hagness, S. (2010). Computational electrodynamics. Boston, Mass: Artech House.

## Slide 45
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
How does FDTD work? – Maxwell’s Curl Equations
Taflove, A., & Hagness, S. (2010). Computational electrodynamics. Boston, Mass: Artech House.

## Slide 46
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
How does FDTD work? – Maxwell’s Curl Equations
Taflove, A., & Hagness, S. (2010). Computational electrodynamics. Boston, Mass: Artech House.

## Slide 47
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
How does Lumerical-FDTD calculate transmittance?
https://support.lumerical.com/hc/en-us/articles/360034405354-transmission-Script-command

## Slide 48
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Why does redshift occur?
Duque, Johan. (2017). Re: Why does the peak of surface plasmon resonance shift to redder, longer wavelength with increasing the refractive index of the medium?. Retrieved from: https://www.researchgate.net/post/Why-does-the-peak-of-surface-plasmon-resonance-shift-to-redder-longer-wavelength-with-increasing-the-refractive-index-of-the-medium/58b60cf6eeae393cf93fdcd3/citation/download
Higher refractive index  Increase in dielectric function  Increase in polarization  Reduction in restoring force  Reduction in resonant frequency  Redshift of the spectrum

## Slide 49
H3 Research
Kushagra Shrivastava
Introduction
Experiments and Methodology
Results and Discussion
Future Works
Liquid Layer
50 nm
(50 + h) nm

## Slide 50
dl / nm | resonant per mode / nm |  |  | 
 | I | II | III | IV
20 | 1.40 | 6.17 | 1.54 | —
30 | 1.40 | 6.17 | 2.03 | —
40 | 0.69 | 6.61 | 3.02 | —
50 | 2.43 | 7.07 | 3.49 | —
60 | 2.77 | 7.02 | 3.96 | —
70 | 2.07 | — | 4.41 | —
80 | 3.09 | — | 4.86 | —
90 | 1.83 | — | 5.29 | 11.2
100 | 2.72 | — | 5.73 | 12.7
110 | 2.03 | 9.66 | 6.61 | 13.5
120 | 3.37 | 10.4 | 7.03 | 13.8
130 | 4.69 | 11.5 | 7.86 | 14.5
140 | 3.66 | 11.6 | 8.23 | 15.3
150 | 3.31 | 12.3 | 9.03 | 15.9
160 | 4.28 | 12.5 | 9.80 | 16.6
170 | 4.26 | 12.2 | 9.20 | 16.2
dl / nm |  |  |  | 
 | I | II | III | IV
20 | 1.40 | 6.17 | 1.54 | —
30 | 1.40 | 6.17 | 2.03 | —
40 | 0.69 | 6.61 | 3.02 | —
50 | 2.43 | 7.07 | 3.49 | —
60 | 2.77 | 7.02 | 3.96 | —
70 | 2.07 | — | 4.41 | —
80 | 3.09 | — | 4.86 | —
90 | 1.83 | — | 5.29 | 11.2
100 | 2.72 | — | 5.73 | 12.7
110 | 2.03 | 9.66 | 6.61 | 13.5
120 | 3.37 | 10.4 | 7.03 | 13.8
130 | 4.69 | 11.5 | 7.86 | 14.5
140 | 3.66 | 11.6 | 8.23 | 15.3
150 | 3.31 | 12.3 | 9.03 | 15.9
160 | 4.28 | 12.5 | 9.80 | 16.6
170 | 4.26 | 12.2 | 9.20 | 16.2

## Slide 51
h / nm | resonant per mode / nm |  |  | 
 | I | II | III | IV
60 | 0.296 | 6.988 | 5.99 | 10.09
80 | 0.8 | 8.8 | 8.81 | 16.82
100 | 3.542 | 10.89 | 8.76 | 14.43
120 | 4.28 | 12.5 | 9.80 | 16.6
140 | 4.33 | 13.91 | 9.8 | 17.7
160 | 6.39 | 15.25 | 11.2 | 19.33
h / nm |  |  |  | 
 | I | II | III | IV
60 | 0.296 | 6.988 | 5.99 | 10.09
80 | 0.8 | 8.8 | 8.81 | 16.82
100 | 3.542 | 10.89 | 8.76 | 14.43
120 | 4.28 | 12.5 | 9.80 | 16.6
140 | 4.33 | 13.91 | 9.8 | 17.7
160 | 6.39 | 15.25 | 11.2 | 19.33

## Slide 52
Refractive index / RIU | Resonant wavelength per mode / nm |  |  | 
 | I | II | III | IV
1.34 | 983.284 | 1089.61 | 1146.02 | 1202.62
1.35 | 984.484 | 1092.19 | 1147.45 | 1203.90
1.36 | 985.686 | 1094.59 | 1149.05 | 1205.11
1.37 | 986.887 | 1096.60 | 1150.65 | 1206.31
1.38 | 987.688 | 1099.00 | 1152.25 | 1207.91
1.39 | 988.942 | 1101.11 | 1154.17 | 1209.09
1.40 | 990.954 | 1103.61 | 1155.54 | 1210.60
FWHM / nm | 2.123 | 3.888 | 3.526 | 12.363